Calibration - 2 . circle: analysis offers

Anet A 8  Plus · Raspberry Pi 3  · BIGTREETECH SKR 2  · Klipper / Mainsail · IdeaMaker 5.5 . 0.8810

Model: Flow_Calibration_Cube_0.4_mm.stl (50 mm 50 mm 50 mm)  Filament: [Raise3D] Premium PLA 1.75 mm

Measurement summary

| Axis | 3 measurement | Average | Deviation | error % |
| --- | --- | --- | --- | --- |
| X | 49.76 / 49.74 / 49.69 | 49.730 | - 0.270 mm | - 0.54 % |
| Y | 49.82 / 49.85 / 49.84 | 49.837 | - 0.163 mm | - 0.33 % |
| Z | 49.78 / 49.80 / 49.74 | 49.773 | - 0.227 mm | - 0.45 % |

The G-code side is correct: bounding box exactly X100 150 / Y100 150; the outer wall course runs from 100.200 to 149.800 (0.2 = half extrusion width), and the last layer is ;LAYER:199 / ;Z:50.000. Thus, the slicer targets exactly 50.000 mm the deficiency is physical, not a G-code error.

Stepper motor step count almost certainly NOT is the wrong one

Steps:

1 . The configurations of X and Y are identical ( rotation_distance : 40 , microsteps : 16  → 80  steps/mm), yet 0.107 mm - rel differ from each other.  A step count- error would screw both equally.

2. Z uses a completely different drive (T8 spindle, rotation_distance: 8  400 step/mm), with an error near 0.45%. Two independent drivetrains cannot coincidentally be identical in proportion.

3 . The gotten value resulting from the rotation_distance : 40  geometry ( GT2 belt 2 mm division × 20  tooth ).errors are discrete: if 16  toothed pulley is were , it would be − 20 % were , not − 0.5 % .  The same applies for Z: the rise of 8 mm.

4 . All three shrink 0.3 – 0.55 % – this is the textbook thermal expansion shrink of PLA ( 0.3 – 0.5 % ).

In short, it's material shrinkage + slight underextrusion, not step count error.

The fan issue is clarified

Based on G- code, the fan not went at maximum :

• ; LAYER : 1  → M106 S64 = 25 %

• ; LAYER : 3  → M106 S153 = 60 %

• then 60 % , no more M106 until the end of printing

So 3 . for layer a there is a jump from 25 % to 60 % – this is caused the sense of “maximumra went”.  not Klipper - error , than is the cooling ramp for IdeaMaker.  For the however 190 °C nozzle, the sudden 60 % cooling too much : destroy the layer adhesion and increases the shrinkage stress.

Offered New Settings

IdeaMaker - the main fixes

| Setup | Current | Offered | Why |
| --- | --- | --- | --- |
| Flow / Filament Compensation # 1 | 94 % | 100 % | The extruder is calibrated (rotation_distance: 35.845), so 94% would be double compensation. It produces a narrower wall (0.376 instead of 0.4), which removes approximately 0.012 mm. |
| Nozzle temperature | 190 °C | 200 – 205 °C | Raise3D Premium PLA factory recommendation approx. 205 °C. 190 °C + 60 % cooling gives low layer adhesion. |
| bed temperature | 50 °C | 60 °C | better grip, less bottom warp. |
| Fan | L 1: 25 % , L3 : 60 % | L1: 0%, then ramp from L6 to L8 to a maximum of 50%. | Instead of a sudden jump, use gradual cooling less shrinkage stress. |

Size compensation

this only finalize after B- test, but the initial values are:

• X: 50  / 49.730  = 100.54 %

• Y: 50  / 49.837  = 100.33 %

• Z: 50  / 49.773  = 100.46 %

Set this in the slicer ( Shrinkage Compensation – Scale Factor ), not ` rotation_distance `- ben . If you burn into the machine, then PETG / ABS / TPU when printing (other shrinkage) again wrong , and destroy the layer height and also probe

Since the X/Y difference (0.11 mm) is greater than the measurement standard deviation, it would be worth checking the X belt tension and pulley grub screw. X is the worst axis, and on the A8 Plus the X belt is the most flexible element.

printer. cfg – amit I would definitely fix it

These not they talk about size problem but real errors are Configuration_Files_Mainsail_Klipper / printer . In file cfg:

1. The bed range mesh is physically unreachable. The mesh_max coordinates are 280,280; with the probe offsets (x_offset: 30, y_offset: 25), the nozzle would need to travel to X=310, Y=305, but position_max is 300. Recommended:

[ bed_mesh ]

mesh_min : 20 , 20

mesh_max : 265 , 265

2 .  old remainder is SAVE_CONFIG block : a [ stepper_z ] position_endstop = 0.300  remained , and the is endstop probe : z_virtual_endstop .  this delete it.

3. BLTouch Z-offset manual value (z_offset: 1.25); the [bltouch] SAVE_CONFIG block is empty, meaning PROBE_CALIBRATE has never been run. This directly affects the Z dimension and the first layer. Instead of paper: PROBE_CALIBRATE  TESTZ  ACCEPT  SAVE_CONFIG.

4 . ` pressure_advance : 0.05 ` only tipp. This affects the geometry of the sarkok - worth calibrating.

next round

A- test – permanent exclusion of the number of steps (without plastic)

G28

G90

G1 X10 F3000

Mark the nozzle position, then:

G1 X210 F3000

Measure the distance between the two positions with a steel ruler or caliper; 200.00 mm 0.2 mm is expected. The same applies to Y. If it matches, rotation_distance is certainly correct and does not need to be modified.

B-test - proportional or constant error? (This is the key question.)

Print a 100mm  × 20mm  × 20mm column next to cube.

• 	If the side of 100 mm is also approx.  0.5 % - kal (approx. 0.5 mm ) short → shrinkage → proportional Scale compensation to correct .

- If every size is short by the same amount (approximately 0.25 mm), regardless of length  extrusion-width / flow error  XY Size Compensation (horizontal expansion) is correct.

Only not can be decided from the 50 mm cube, so given is the misleading result of the first round.

Only then , if A- test is really showed a machine error

The values would be These - but based on the results bellow :

# only if mechanical problem verified!

[ stepper_x ] rotation_distance : 39.784

[ stepper_y ] rotation_distance : 39.869

[ stepper_z ] rotation_distance : 7.9637

Where is 94% set?

It is not in the template Advanced Settings. Screenshot 15 covers the entire tab, and neither location contains 94%.

A ; Filament Compensation # 1 : 94.000  and M221 T0 S94 . 00 a comes from filament definition, not from slicing template. The header of the G-code tells you which one:

; Filament Name # 1 : [ Raise3D ] Premium PLA 1.75mm

; Filament Compensation # 1 : 94.000

This is [Raise3D] Premium PLA 1.75 mm, stored in the filament named PLA; the Diameter, Density, and Type fields are next to it.

Set to 100 %

IdeaMaker main window → right-hand panel Filament drop-down next to the edit ( gear ) icon , or in the top menu Printer → Filament Settings …

In the window that opens, select [ Raise3D ] Premium PLA 1.75mm filamentet , and rewrite the field Compensation / Filament Compensation 94  → 100 .

Check after reslicing - the G- code header should read this:

; Filament Compensation # 1 : 100.000

M221 T0 S100 . 00

two flow layers are multiplied together

I saw Amit on the Quality tab (this is the second layer, per feature):

| Flowrate | Value |
| --- | --- |
| Outer Shell Flowrate | 100.0 % |
| Inner Shell Flowrate | 90.0 % |
| Infill Flowrate | 90.0 % |
| Base / Solid Fill Flowrate | 95.0 % |
| Top / Bottom Surface | 120.0 % |

The actual amount of material = Filament Compensation feature Flowrate. For the external wall (which defines the size), it is currently 94% 100% = 94%. Therefore, the size-reducing under-extrusion comes entirely from the 94% filament setting; setting it to 100% cancels exactly this effect.

For # 2 : 90.000 a second extruder filament , print no matters.

offered settings

Quality tab, right side - "Shrinkage Compensation"

currently 100.00 % :

Scale Factor X: 100.54

Scale Factor Y: 100.33

Scale Factor Z: 100.46

This shrinkage compensation is correct place – not to rotation_distance. left-hand “ Dimensional Compensation → XY Size Compensation for Contours ” however constant mm offset -  then use if B- test constant, showed not proportional error.

Cooling tab - “ Fan Control ” lista

Currently:

| Layer | Fan Speed |
| --- | --- |
| 2 | 25 |
| 4 | 60 |

The G-code is based on 0; LAYER: numbering explains why M106 S64 appears for layer 1 and M106 S153 for layer 3, so it matches.

Recommended softer ramp:

| Layer | Fan Speed |
| --- | --- |
| 2 | 20 |
| 5 | 35 |
| 8 | 50 |

Temperature tab

• Heated Bed Temperature : 50  → 60 °C

• Primary Extruder : 190  → 200 – 205 °C

Order keep this in mind

First set flow to 100 print the cube again before entering Scale Factor - okat - otherwise you would also compensate for the flow improvement and miss the mark.

1 .  Filament Compensation 94  → 100

2 . Fix temperatures and fan ramp

3. PROBE_CALIBRATE + SAVE_CONFIG (instead of paper) the detailed description follows in the next section.

4 . A- teszt (mechanical Step Count Check)

5 . Reprint: 50 mm column cube + 100  × 20  × 20 mm column (B- test )

6 .  Only then finalize Shrinkage Compensation Scale Factor

Z- offset calibration step by step

The PROBE_CALIBRATE  TESTZ  ACCEPT  SAVE_CONFIG process in detail.

Preparation

Z- offset is temperature dependent, so do need for operating temperature, with a pure nozzle.

1 .  Mainsail → Dashboard → set temperatures (from or console):

M140 S60

M104 S200

M190 S60

M109 S200

2 . While heats , clean the tip of the nozzle (copper brush or tweezers , careful – hot). The attached filament residue directly falsifies the offsetet.

3. Extrude a small amount of filament, then wipe away the ooze. If PLA drips continuously and interferes with the paper test, temporarily reduce the nozzle to M104 S170 during measurement the difference in thermal expansion is negligible (approximately 0.01 mm).

The calibration is menete

Mainsail → Console tab and enter:

G28

PROBE_CALIBRATE

In Klipper :

• measures from BLTouch – the current point

Then move the nozzle to the same point (x_offset: 30 / y_offset: 25), from the head position 150,150 to 120,125 approximately the center of the bed, which is ideal.

• and enters manual measurement mode.

1 . method - Mainsail dialog box (simpler)

After PROBE_CALIBRATE in Mainsail automatikusan appears a Z- offset window + / - buttons ( 0.01  / 0.05  / 0.1  / 1 mm ), as well as ACCEPT and ABORT button .  You can also do With this by clicking, type not need a command.

2 . method - TESTZ commands

Place a a normal sheet of paper (approx. 0.1 mm ) under the nozzle and zoom down:

TESTZ Z= -1

TESTZ Z= -0.5

TESTZ Z= -0.1

TESTZ Z= -0.05

If you went over (the paper stricked), go back :

TESTZ Z= +0.05

There is also a halving aid: between the known lower and upper limits, it jumps to the midpoint.

TESTZ Z=-

TESTZ Z=+

The goal: the paper is still just sliding, but you are already pulling with noticeable friction. Don't stuck in.

Completion

ACCEPT

SAVE_CONFIG

• ACCEPT calculates the new z_offset .

• SAVE_CONFIG will enter into the config and restart Klippert (this is normal).

Checking

After reboot, printer.cfg should end with an otherwise empty #*# [bltouch] block containing the value:

#*# [ bltouch ]

#*# z_offset = 1 . xxx

This overrides the manually entered z_offset : 1.25 in the [ bltouch ] section - so you know , that are really completed .

Fine tuning on the first layer

The paper test only is a good place to start. The actual setting is done during printing:

1 . Start a large , single layer test.

2 . During printing, adjust in Mainsail a Z offset + / - buttons ( or SET_GCODE_OFFSET Z_ADJUST = -0.01  MOVE = 1 ) until the first layer is nicely connected, slightly flattened.

3 . If ok , burn in the found value:

Z_OFFSET_APPLY_PROBE

SAVE_CONFIG

This adds live offsetet to probe z_offset - hez, so the next time is already good.

Two important comments

Correction to the previous statement: I wrote above azt from nose #*# [ stepper_z ] position_endstop = 0.300 s , that "collides" with the virtual endstoppal.  More precisely: probe : z_virtual_endstop when using Klipper this the field simply figyelmen outside leaves , not cousing error.  Only misleading residue - safely can be deleted but not is urgent.

However, bed mesh calibration is urgent: if you run BED_MESH_CALIBRATE after the Z-offset, the current mesh_max: 280,280 would cause the nozzle to move out of bounds, because it would need to travel to X=310 / Y=305, beyond position_max: 300. This must first be corrected to 265,265.

BLTouch and bed mesh calibration

Complete this calibration before the first print. The BLTouch Z offset defines the vertical distance between the nozzle and the probe trigger point. The bed mesh maps small height variations across the build plate.

1. Preparation and safety

1. Clean the nozzle and build plate. Do not leave plastic on the nozzle tip.

2. Make sure the BLTouch is firmly mounted, its pin moves freely, and no cable can snag.

3. Turn on the printer and open the Mainsail Console.

4. Keep Emergency Stop within reach. If Z moves down and the BLTouch does not stop it, press Emergency Stop immediately.

2. Test the BLTouch

Run these commands one at a time in the Console:

BLTOUCH_DEBUG COMMAND=reset

BLTOUCH_DEBUG COMMAND=pin_down

BLTOUCH_DEBUG COMMAND=pin_up

The pin must deploy and retract. Next, deploy the pin and gently push it upward by hand:

BLTOUCH_DEBUG COMMAND=pin_down

QUERY_PROBE

With the pin deployed, the result must be open. Push the pin up and run QUERY_PROBE again; the result must be TRIGGERED. If this does not work, do not home the printer. Check the wiring and the sensor_pin/control_pin settings in printer.cfg.

3. Test Z homing

1. Move the printhead so that the BLTouch is above the build plate.

2. Run G28. The printer homes X and Y first, then homes Z near the center of the bed.

3. During the Z movement, gently touch the BLTouch pin. Z must stop immediately. If it does not stop, use Emergency Stop.

4. If the test succeeds, run G28 again and allow the BLTouch to complete Z homing against the bed.

G28

4. Calibrate the BLTouch Z offset

1. Use conditions close to normal printing: heat the bed to the temperature used for the material, then wait a few minutes. Keep the nozzle clean; for a safe paper test, do not leave hot plastic on its tip.

2. Run G28, followed by PROBE_CALIBRATE.

3. Place a sheet of ordinary paper under the nozzle.

4. Move down with TESTZ Z=-1, then TESTZ Z=-0.1. Near the paper, use smaller TESTZ Z=-0.01 steps.

5. If the nozzle moves too low, raise it with TESTZ Z=0.01. The height is correct when the paper still moves but lightly drags against the nozzle.

6. Run ACCEPT. The result is not accepted without this command.

7. Run SAVE_CONFIG. Klipper restarts and automatically saves the z_offset value in the SAVE_CONFIG block at the end of printer.cfg.

G28

PROBE_CALIBRATE

TESTZ Z=-0.1

TESTZ Z=-0.01

ACCEPT

SAVE_CONFIG

Do not edit the SAVE_CONFIG block manually. Pin and offset settings in the normal [bltouch] section of printer.cfg can be edited manually, but Klipper manages the calibrated z_offset value.

5. Calibrate the bed mesh

A bed mesh does not replace mechanical bed leveling. First adjust the bed to be as level as possible, then create the mesh.

1. Heat the bed to the temperature normally used for printing, then wait a few minutes for thermal expansion to stabilize.

2. Run G28.

3. Run BED_MESH_CALIBRATE. With the current printer.cfg settings, the BLTouch measures a 5 x 5 grid, for a total of 25 points.

4. Wait until all measurement points are complete.

5. Run SAVE_CONFIG. Klipper restarts and saves the mesh under the name default.

G28

BED_MESH_CALIBRATE

SAVE_CONFIG

6. Use the saved mesh

BED_MESH_CALIBRATE measures all points only during calibration. For normal printing, load the saved mesh. Add this command to the IdeaMaker Start G-code after G28:

BED_MESH_PROFILE LOAD=default

Important: G28 may clear the active mesh, so the load command must always come after G28.

7. Verification and recalibration

1. Print a first-layer test and make small Z-offset corrections in Mainsail if necessary.

2. After changing the Z offset, save it with SAVE_CONFIG.

3. Repeat PROBE_CALIBRATE after changing the nozzle, hotend, or BLTouch mounting.

4. Create a new bed mesh after adjusting the bed, BLTouch, or printer mechanics, or if first-layer height still varies across the bed.